## Slide 1
Droplet evaporation rate analysis on hot superhydrophobic surface

## Slide 2: Snapshot of water droplet on substrate
0.6mm
It looks like Cassie state from side view point

## Slide 3: Large sliding angle

## Slide 4: Energy balance during the evaporation process
Heat transfers from the hot substrate into the water droplet,
leading to the temperature increase of the water droplet. The heat is
released to the ambient by means of convection, radiation and evaporation.

## Slide 5
Abdullah A, Berkir S, Haider A, Droplet Heat transfer on Micropost Arrays With Hydrophobic and Hydrophilic Characteristics. Journal of Heat Transfer. Vol. 140/ 072402-1.

## Slide 6: Thermal resistance of the substrate
Thermal resistance of water vaper is much larger than all the others

## Slide 7: Thermal constriction/spreading resistance
Thermal constriction resistance exists when heat flows from a large region into a narrower region.
Thermal spreading resistance exists when heat flows from a narrow region into a larger cross sectional area.

## Slide 8: Water droplet evaporation

## Slide 9: 16um diameter 40um periodicity 20um micropillar height
100C° hot plate --- 89C° droplet
110C° hot plate --- 96C° droplet
120C° hot plate --- 100C° droplet
130C° hot plate --- 100C° droplet

## Slide 10: 20um diameter 60um periodicity 40um micropillar height
100C° hot plate --- 80C° droplet
110C° hot plate --- 85C° droplet
120C° hot plate --- 90C° droplet
130C° hot plate --- 94C° droplet

## Slide 11: 20um diameter 50um periodicity 20um micropillar height
100C° hot plate --- 87C° droplet
110C° hot plate --- 94C° droplet
120C° hot plate --- 100C° droplet
130C° hot plate --- 100C° droplet

## Slide 12: 20um diameter 50um periodicity 40um micropillar height
100C° hot plate --- 87C° droplet
110C° hot plate --- 94C° droplet
120C° hot plate --- 100C° droplet
130C° hot plate --- 100C° droplet

## Slide 13: 20um diameter 40um periodicity 40um micropillar height
100C° hot plate --- 92C° droplet
110C° hot plate --- 99C° droplet
120C° hot plate --- 100C° droplet
130C° hot plate --- 100C° droplet

## Slide 14: 20um diameter 40um periodicity 40um micropillar height
120C° hot plate --- 105C° droplet
130C° hot plate --- 110C° droplet

## Slide 15: Mask design
1
2
3
4
5
6
7
8
9
#1 20um diameter, 70um periodicity
#2 20um diameter, 80um periodicity
#3 20um diameter, 90um periodicity
#4 20um diameter, 100um periodicity
#5 20um diameter, 110um periodicity
#6 20um diameter, 120um periodicity
#7 16um diameter, 80um periodicity
#8 16um diameter, 100um periodicity
#9 16um diameter, 120um periodicity

## Slide 16: Mask design

## Slide 17: Mask design

## Slide 18: Mask design

## Slide 19: Mask design

## Slide 20: Mask design

## Slide 21: Mask design

## Slide 22: Mask design

## Slide 23: Mask design

## Slide 24: Mask design

## Slide 25: Critical contact angle
Diameter (um) | Periodicity (um) | Critical CA with 40um height (°) | Critical CA with 20 um height (°)
20 | 30 | 100 | 108
20 | 40 | 109 | 120
20 | 50 | 117 | 129
20 | 60 | 124 | 136
20 | 70 | 130 | 141
20 | 80 | 135 | 146
20 | 90 | 139 | 149
20 | 100 | 142 | 152
20 | 110 | 145 | 154
20 | 120 | 148 | 156