## Slide 1: Substrate
Silicon substrate with micropillar:
Diameter 20um; periodicity 40 um; height 40um.
Fluorinated silane (Trichloro(1H,1H,2H,2H-perfluorooctyl)-silane, Sigma Aldrich) is conformally coated on the silicon substrate through chemical vapor deposition process for about 1 hour. Then put the substrate on hot plate with 90 °C for about 1 hour.

## Slide 2: Contact Angle and Contact radius
100 °C hot plate
110 °C hot plate

## Slide 3: Droplet volume and spherical cap assumption
100 °C hot plate
110 °C hot plate

## Slide 4: Evaporation equation
Droplet evaporation equation based on the thermal circuit model is:
where L is latent heat, rho is water density; Rtotal and Rthermal are thermal resistance related to substrate structure; rc is contact angle. Assuming spherical cap model
in CCA model as is independent of time.

## Slide 5: Droplet evaporation in CCR model
When droplet evaporation model transfer from CCR model to CCA model, contact radius begins to decrease rapidly and contact angle maintains almost constant. At this time the droplet volume is small enough and spherical cap assumption is suitable.
Droplet volume at this moment can be calculated as:
Time for CCR model can be calculated as：

## Slide 6: Droplet evaporation in CCA model
In CCA model, the droplet volume is small and we can use spherical cap assumption to calculate the droplet volume.
At this time, droplet contact angle keeps constant and contact radius decreases with time. Thus the derivation of volume respect to time can be calculate as:
Also, we know:
Combine these two expressions, we get:
Expression for contact radius in CCA model is：

## Slide 7: Expression for contact radius in the whole evaporation process
Now we get the expression for the contact radius in CCA model and CCR model. If we ignore the mixed model in the very end of the evaporation, the expression contact radius is:
where
Time for CCA model can be assumed as:

## Slide 8: Predicted contact radius
100 °C hot plate
110 °C hot plate

## Slide 9: Volume calculated by predicted contact radius
100 °C hot plate
110 °C hot plate

## Slide 10: Ratio of CCR model and CCA model
Now we know the evaporation time for CCR model and CCA model:
The ratio of CCR model and CCA model is related to droplet initial volume, initial contact radius and CCA model contact angle. It is independent of temperature and substrate structure.

## Slide 11: Normalized evaporation data

## Slide 12: Prediction model
Assuming we know the droplet volume , contact radius , temperature , contact angle in CCA model is equal to receding contact angle , then we can predict the droplet evaporation process on a given substrate.
Time for CCR model and CCA model: